## Slide 1
Advanced Drug Delivery Reviews 54 (2002) 3–12
Hydrogels for biomedical applications
Allan S. Hoffman

## Slide 2
Hydrophilic polymers used to synthesize hydrogel matrices
Natural polymers and their derivatives (±crosslinkers)
Anionic polymers: hyaluronic acid, alginic acid, pectin, carrageenan, chondroitin sulfate, dextran sulfate
Cationic polymers: chitosan, polylysine
Amphipathic polymers: collagen (and gelatin), carboxymethyl chitin, fibrin
Neutral polymers: dextran, agarose, pullulan, scleroglucan.
Synthetic polymers (±crosslinkers)
Polyesters: PEG-PLA-PEG, PEG-PLGA-PEG, PEG-PCL-PEG, PLA-PEG-PLA..
Other polymers: PEG-bis-(PLA-acrylate)…
Combinations of natural and synthetic polymers
P(PEG-co-peptides), alginate-g-(PEO-PPO-PEO), P(PLGA-co-serine), collagen-acrylate, alginate-acrylate, P(HPMA-g-peptide), P(HEMA/Matrigel…….

## Slide 3
Methods for synthesizing physical and chemical hydrogels
Physical gels
Warm a polymer solution to form a gel (e.g., PEO-PPO-PEO block copolymers in H2O)
Cool a polymer solution to form a gel (e.g., agarose or gelatin in H2O)
‘Crosslink’ a polymer in aqueous solution, using freeze–thaw cycles to form polymer microcrystals
(e.g., freeze–thaw PVA in aqueous solution)
Lower pH to form an H-bonded gel between two different polymers in the same aqueous solution (e.g., PEO and PAAc)
Mix solutions of a polyanion and a polycation to form a complex coacervate gel (e.g., sodium alginate plus polylysine)
Gel a polyelectrolyte solution with a multivalent ion of opposite charge (e.g., Na alginate + Ca 2+ )
Chemical gels
Crosslink polymers in the solid state or in solution with:
Radiation (e.g., irradiate PEO in H2O)
Chemical crosslinkers (e.g., treat collagen with glutaraldehyde or a bis-epoxide)
Multi-functional reactive compounds (e.g., dextran + dicarboxylic acids)
Copolymerize a monomer+crosslinker in solution (e.g., HEMA+EGDMA)
Copolymerize a monomer+a multifunctional macromer (e.g., bis-methacrylate terminated PLA-PEO-PLA+photosensitizer
+visible light radiation)
Polymerize a monomer within a different solid polymer to form an IPN gel
Chemically convert a hydrophobic polymer to a hydrogel (e.g., partially hydrolyse PVAc to PVA or PAN to PAN/PAAm/PAAc)

## Slide 11
Advanced Drug Delivery Reviews 54 (2002) 13–36
Novel crosslinking methods to design hydrogels
W.E. Hennink, C.F. van Nostrum

## Slide 12: Reaction of dextran with GMA

## Slide 13: Structures of (A) dex-MA, (B) dex-HEMA and (C) dex-(lactate) -HEMA

## Slide 15: Aldehyde-mediated crosslinking of polymers containing alcohol, amine or hydrazide groups (R represents the polymer chains, X is any spacer e.g. (CH ) in the case of glutaraldehyde)

## Slide 16: Passerini and Ugi condensation reactions

## Slide 18: Preparation of PEG hydrogels crosslinked by polyrotaxanes

## Slide 19: Polymer 49 (2008) 1993-2007
Hydrogels in drug delivery: Progress and challenges
Todd R. Hoare, Daniel S. Kohane

## Slide 20: Mechanism of in situ physical gelation driven by hydrophobic interactions

## Slide 21: Chemical structures and abbreviations of common thermo-gelling hydrophobic blocks.

## Slide 22: Mechanisms of in situ physical gelation based on charge interactions with an oppositely-charged polymer or an oppositely-charged small molecule cross-linker

## Slide 23: In situ physical gelation via hydrogen bonding interactions between geometrically-compatible biopolymers (methylcellulose and hyaluronic acid); the hydrogen bonds break under shear.

## Slide 24: Mechanism of in situ physical gelation via stereocomplexation between L- and D- lactide polymer chains

## Slide 25: Mechanism of in situ physical gelation via the formation of a supramolecular complex between poly(ethylene oxide) (PEO) and cyclodextrin

## Slide 26: Typical in situ-cross-linking chemistries: (a) reaction of an aldehyde and an amine to form a Schiff base; (b) reaction of an aldehyde and hydrazide to form a hydrazone; (c) Michael reaction of an acrylate and either a primary amine or a thiol to form a secondary amine or a sulfide.

## Slide 27: Physical (a) and chemical (b) strategies for enhancing the interaction between a loaded drug and a polymeric gel to slow drug release.

## Slide 28: Formation and structure of semi- and full interpenetrating polymer networks (IPN).

## Slide 29: Drug diffusion control by surface-modifying a hydrogel with an environmentally-responsive polymer graft.

## Slide 30: ‘‘Plum pudding’’, composite hydrogels containing drug encapsulated in a secondary controlled release vehicle (e.g. microparticles, nanoparticles, microgels, liposomes, micelles). D1 and D2 represent the diffusion coefficients of drug out of the hydrogel (D1 =release from secondary release vehicle; D2 = diffusion through hydrogel).

## Slide 31: Strategies for hydrophobic drug delivery via hydrogels (a) random copolymerization of a hydrophobic monomer; (b) grafting of hydrophobic side-chains; (c) incorporation of cyclodextrin.