## Slide 1
Dilla University
Department of Physics(Laser Spectroscopy)
Alemayehu Kiros(PhD)
A multi-analytical study of the stone biodeterioration at a UNESCO world heritage site: the rock-hewn churches of Lalibela, Ethiopia

## Slide 2: A multi-analytical study of the stone biodeterioration at a UNESCO world heritage site: the rock-hewn churches of Lalibela, Ethiopia
Outline of the Presentation
1.0 Introduction
1.1 Objective
1.2 Literature review
2.0 Theoretical Background
3.0 Materials and Methods
4.0 Results and Discussion
5.0 Conclusion and Recommendation

## Slide 3: 1.0 Introduction

## Slide 4: 1.0 Introduction
Cultural heritage conservation is an important issue that has a great impact on several aspects of our life, from cultural to economical ones
Nowadays, the conservation of our cultural heritage is one of the main world concerns, like the rock- hewn churches of Lalibela
We are proud of these treasures, but they are affected by:
environment physical (temperature and humidity),
human (pollutant releases, wood burning and/or solid waste) impact,
biological factors

## Slide 5
External view of Bete Gebriel-Rufael
Internal view of Bete Gebriel-Rufael
Top view
External view of Bete Giyorgis
External view of Bete Michael Golgotha

## Slide 6
This exposure has resulted in the severe degradation of the churches, most of which are now considered to be in a critical condition.
the damage assessment and, in general, the control of the conservation status of a monument is a complex issue that involves the investigation and measurement of many parameters.
1.1 Objective
The aim of this work was,
to study in detail for the first time, using a multi-analytical approach combining Optical Microscopy (OM), Backscattered Variable Pressure Scanning Electron Microscopy + Energy Dispersive X-ray Spectroscopy (VP-BSEM + EDS), Powder X-ray Diffractometry (PXRD), LIBS, FTIR, Raman spectroscopy and standard Microbiological techniques, the bio-deterioration processes and products associated with lichenous coatings on a “unusual” building stone such as the Lalibela volcanic scoria with a view to contributing to a better conservation strategy for this World Heritage site.

## Slide 7: 1.2 Literature review
Rock samples from the Lalibela have been analyses using SEM-EDS (Delmonaco et al., 2009; Renzulli et al., 2005). The analyses showed that most of them are filled by late-stage and post-magmatic hydrothermal zeolites such as analcite, heulandite, natrolite±thomsonite and calcite.
Rock samples from the Lalibela have been characterized using XRD (Delmonaco et al., 2009; Renzulli et al., 2005). The study was carried out determine the presence of smectite group minerals in the whole rocks, which also identified hematite, zeolites and calcite as the main secondary minerals.
The distribution of weathering products on the surface is generally characterized by spectroscopic measurements.

## Slide 8: 2.0 Theoretical Background

## Slide 9: Scanning electron microscopy with energy dispersive spectrometry (SEM-EDS)
The SEM has a
large depth of field, which allows a large amount of the sample to be in focus at one time and produces an image that is a good representation of the three-dimensional sample.
high resolution, which means that closely features can be examined at a high magnification.
Magnification Depth of Field Resolution
SEM 10x – 3000000x 4mm – 0.4mm 1-10nm

## Slide 10: Basic principles Electron Beam and rock sample Interactions

## Slide 11
Secondary Electrons (SE)
Backscattered Electrons (BSE)
Produced by inelastic interactions of high energy electrons with valence (or conduction) electrons of atoms in the rock samples, causing the ejection of the electrons from the atoms. These ejected electrons with energy less than 50eV are termed "secondary electrons".
Secondary electron emission is concentrated around the primary spot, and constitutes a high resolution source of near-surface information
Production of SE is very topography related
BSE are produced by elastic interactions of beam electrons with nuclei of atoms in the rock samples and they have high energy and large escape depth.
Higher Z, more BSE emitted

## Slide 12: Infrared Spectroscopy
IR deals with the interaction of infrared radiation with matter
When radiation passes through a sample (solid, liquid or gas), certain frequencies of the radiation are absorbed by the molecules of the substance leading to the molecular vibrations.
IR spectroscopy is primarily used to identify bond types, structures, and functional groups in organic and inorganic compounds
Molecules absorb IR radiation at frequencies related to their unique compositions, structures and the numbers, types, strengths and position of their bands.
Electromagnetic Radiation
The propagation of electromagnetic radiation in a vacuum is constant for all regions of the spectrum (= velocity of light):
c =  × 
1 Å = 10 –10 m 1 nm = 10 –9 m 1 m = 10 –6 m
Another unit commonly used is the wavenumber, which is linear with energy:

## Slide 13
Vibrational Modes
The vibration of any structure is analyzed in terms of the degrees of freedom which the structure possesses.
  Number of possible modes
  Nonlinear molecule: 3N – 6
    Linear molecule: 3N – 5
  3 degrees of freedom – i.e., 3 coordinates in space
  3 translations and 3 rotations account for 6 motions of molecule
  Rotation about center bond in linear molecule is indistinguishable
  Remaining degrees of motion represent vibrational motion (i.e., number of vibrations within the molecule)

## Slide 14
Types of Molecular Vibrations: Vibrations fall into the basic categories of stretching and bending.
A stretching vibration involves a continuous change in the interatomic distance along the axis of the bond between two atoms.
Bending vibrations are characterized by a change in the angle between two bonds and are of four types:
scissoring,
rocking,
wagging, and
twisting.

## Slide 15
Molecule of water
3N-6  3*3-6 = 3 vibrational states
which results in three absorption bands in IR and Raman.
The number of stretching vibrations is N-1 and
the number of bending vibrations is 2N-5.
Stretching vibrations  3-1 = 2: symmetric stretching of the H-0 bonds and asymmetric stretching of the H-O bonds
Bending vibration  2*3-5 = 1: 1 scissors bending of the HOH structure.

## Slide 16: Raman Spectroscopy
  Basic Principals of Raman Spectroscopy:
Part of the radiation is scattered by molecules when the radiation passes through sample
Three types of scattering occurs
Rayleigh scattering
Stokes scattering
Anti-Stokes scattering

## Slide 17: Classical Raman Physics
Interaction between electric field of incident photon and molecule
  Electric field oscillating with incident frequency ωi:
  Induces molecular electric dipole (µ):
    Proportional to molecular polarizability, 
  -ease with which the electron cloud around a molecule can be distorted
  -Polarization results in nuclear displacement

## Slide 18
For small distortions, polarizability is linearly proportional to the displacement
Resultant dipole:
Term 1 describes the Rayleigh scattering, Term 2 describes the anti-Stokes Raman scattering resulting in the generation of a photon of higher frequency (higher energy) than the incident photon and Term 3 describes the Stokes Raman scattering where a photon of a lower frequency (lower energy) is generated than the incident photon.

## Slide 19: Laser Induced Breakdown Spectroscopy (LIBS)
The process: Laser ablation
Laser interaction with matter always involves an energy exchange. The Laser energy is partially:
Reflected, Scattered
Absorbed
Re-Emitted
Transmitted

## Slide 20: The process: Plasma formation
The laser pulse strikes the sample surface(a)
The energy absorbed is rapidly converted into heat and causes the sample to locally melt
the laser beam contains enough energy to induce vaporization and fragmentation(b)
large number of electrons, ions and excited atoms are present in the vapor and absorb part of the laser energy leading to a breakdown in the vapor and its ionization (c) The emission detected in this phase is When a free electron is decelerated in the presence of a strong electromagnetic field (Bremsstrahlung) and the recombination processes

## Slide 21
De-excitation of ions and neutrals lead to the emission of characteristic photons, a very important point that allows us to determine the concentration of the elements in the plasma with the LIBS technique (d).
aggregates and clusters due to the decrease in temperatures (e)
deposited around the crater along with the molten material created by the laser melting (f).
(Vadillo et al., 2010)

## Slide 22: The process: Local Thermal Equilibrium (LTE)
Plasma parameters
The characteristic properties of plasma are excitation temperature and electron density.
Initially, the plasma temperature is very high (typically T > 30000K), and auto-ionization is dominant
Fast collisional processes bring the plasma to the conditions of LTE (Local Thermal Equilibrium)where the electrons have the same
Kinetic energy (Maxwell-Boltzmann distribution law) : electron temperature. This energy is associated the motion of the electrons. In the case of plasma, it defines the energy of the electrons that obey the Maxwell distribution law i.e. the Maxwellian velocity distribution.
Internal energy (Boltzmann law): excitation temperature. Elements (atoms, ions or molecules) in the plasma have the ability to access higher energy configurations as the temperature increases. The population amongst these excited configurations obey the Boltzmann law characterized by the excitation temperature.
Ionization energy (Saha law): ionic temperature. Saha’s law is used to describe the population distribution among successive ionization degrees within the plasma i.e. the distribution of the same element in different ionization stages.

## Slide 23
Integrated line intensity(Temperature Determination)
Local Thermal Equilibrium (LTE) assumption (all species are at the same temperature)
aα system constant (optical efficiency, ...)
Ne species number density in the plasma
Aki transition rate
gk degeneracy
Uα (T) partition function

## Slide 24: 3.0 Materials and Methods

## Slide 25: Table 3. 1 Sample Analyzed and their locations
Location | Sample name | Wall (surface) | Sample type analyzed | 
 |  |  | Rock | Encrustation (pellets)
Bete Gebriel Rufael Bete Giyorgis Bete Mikael Golgotha Tunnel in front of Bete Amanuel North side of Bete Giyorgis | BGR-E BGR-I BG-E BGM-I BMG-E BAT-E BAT-L BGN-E BGN-L | External Internal External Internal External External External External | basalt tuff basalt basalt basalt tuff basalt basalt | X X X X X

## Slide 26: SEM-EDS
(I)- SEM-EDS investigation was carried out by a Variable Pressure HITACHI S3700N Scanning Electron Microscope interfaced with a Bruker Quantax microanalysis system(at HERCULES Laboratory University of Évora, Évora, Portugal).
The Quantax system was equipped with a Bruker AXS X-Flash®Silicon Drift Detector (129 eV Spectral Resolution at FWHM—Mn Kα).
Standardless PB/ZAF quantitative elemental analysis was performed using the Bruker ESPRIT software.
The operating conditions for SEM-EDS analysis were as follows:
backscattered electron mode (BSEM), SE
20 KV accelerating voltage, 30KV-HV
7.9-14.7 mm working distance(WD = the distance the sample is from the objective lens),
Samples were coated with a thin layer of carbon in order to avoid charging effects.
The carbon coating was obtained using an Emitech sputter coater K550 unit, a K 250 carbon coating attachment and a carbon cord at a pressure of 1x10-2 mbar in order to produce a carbon film with a constant thickness of about 3.0nm.
These conditions have proven optimal to investigate the interface decay patinas/substrate in a variety of historic materials.
Notes: When a SEM is used, the electron-optical column and sample chamber must always be at a vacuum.
If the column is in a gas filled environment, electrons will be scattered by gas molecules which would lead to reduction of the beam intensity and stability.
2. Other gas molecules, which could come from the sample or the microscope itself, could form compounds and condense on the sample. This would lower the contrast and obscure detail in the image.

## Slide 27: Fourier transform infrared spectroscopy (FTIR)
FTIR characterization was performed using The Perkin Elmer Spectrum 65 Spectrum BX FTIR (at Addis Ababa University, Department of chemistry, Ethiopia) was used.
For room-temperature measurements, we used Mercury Cadmium Telluride (MCT) detector for mid-IR spectra.
The beam splitters used were KBr for the mid-IR region 4000 to 400 cm-1 and the resolution was 4cm-1.
The moving mirror velocity 0.6cm/s and bi-directional Interferogram were used.
Samples preparation
Pelleting
2 mg ground sample is mixed with 40 mg of dry KBr powder
Mixture is compressed under very high pressure
Small disk with very smooth surfaces forms (looks like glass)

## Slide 28: Micro-Raman spectroscopy
Micro-Raman characterization was performed using a Renishaw 2000 µ-Raman instrument equipped with a Peltier refrigerator-cooled charge-coupled device (CCD) camera in conjunction with a Leica optical microscope system(at CNR, Institute for the Study of Nanostructured Materials Research Area of ​​Rome 1 - Montelibretti – Italy).
The laser was focused on the sample through a x 100 or x 50 objective lenses.
The excitation light was the 514.5nm line of an Ar+ laser and a 785nm line of a diode laser with laser power in the range of 10-60μW.
Care was taken to avoid sample damage and the typical spectrometer resolution was about 2 cm−1.

## Slide 29
Collecting Optics
Spectrometer
Mirror
Focusing Lenses
delay generator
(Quantel, Twins Ultra 200), emitting 6.5ns long pulses at 1064nm, Nd:YAG Laser
PDA
beam diameter= 6 mm
f=75 mm
E=210mJ
integration time=30ms
Delay time= 4µs
Laser Induced Breakdown Spectroscopy (LIBS)
(ENEA, FIS-LAS, V. E. Fermi 45, Frascati (RM), Italy)
Notes: the focal position of the lens system is wavelength dependent. This is due to the dependence of the refractive index of optical materials on wavelength. For example, for quartz, the refractive index decreases with increased wavelength so that the focal length will increase with increased wavelength. An advantage of a mirror system is that all wavelengths will be focused at the same position

## Slide 30
The plasma emission was collected by two optical systems:
radiation reflected by the pierced mirror and focused onto one fiber bundle by quartz,
two quartz lenses, was mounted at angle of about 45° with respect to the laser axis.
At the other end, the bundle was separated into single fibers, and each of them was connected to one of the five spectrometer channels (Stellar Net)
Channels 1-4 have 0.1 nm spectral resolutions and cover spectral range 200-600nm.
Channel 5 has lower resolution (0.2 nm) and covers the spectral interval 600-800 nm.
Each channel is equipped with a 2048 Photo-Diode Array, and was triggered externally by an optical trigger.
The detectors do not allow for time resolved measurements and
the minimum integration time, here used, was 30ms
The best LIBS signal from basaltic samples was obtained for the acquisition from the laser pulse corresponding to 4µs.
This delay, produced by signal/delay generator (Quantum Composer 9600+) was used in all the measurements.
After one laser shot the whole spectrum was saved for further analysis by custom written programs under Labview
This approach allows monitoring of shot-to-shot variations in the spectral intensities and also the depth profiling.
Samples preparation
The rock samples, cut to 1×1 cm2 large blocks, were directly interrogated by the laser both on the weathered surface and on the bulk material (lateral cut)
The weathered deposits scratched from the surfaces were first pressed pellets into pellets and then analyzed by LIBS

## Slide 31
4.0 Results and Discussion
4.1 Multi-analytical Approach to Investigate Stone Biodeterioration
4.2 FTIR and Raman Spectroscopic Analysis of Clay Minerals
4.3 Analysis of Rock Samples Using Laser-Induced Breakdown Spectroscopy

## Slide 32: 4.1 Multi-analytical Approach to Investigate Stone Biodeterioration

## Slide 33
-OM,BSEM(rock texture) -BSEM(vesicle-filling) -BSEM(bulk rock) -BSEM-Biodeterioration - (LV-SEM image) microbiological contamination and -XRD analysis
The rock texture is characterised by abundant vesicles and open voids readily visible under both OM and BSEM examination
occupying about 40-50% of the stone volume
This is reflected in the stone
high porosity (ranging from 13.5 to 36% -average 28%)
low apparent density (γd ranging from 1.75 to 1.99g/cm3 - average 1.83g/cm3)
indicative of natural stone weathering mechanisms active during the Lalibela basaltic scoria geological history.

## Slide 34
Figure4. 1 Petrography-OM. Highly vesicular basaltic scoria of low porphyritic index with vesicles filled with euhedral zeolites and microphenocrysts of clinopyroxenes in a microlitic groundmass
Fig.4.2a) general view of the volcanic basaltic scoria underneath a lichenous patina (bottom right) highlighting the presence of microphenocrysts of clinopyroxenes and Fe-Ti rich oxides in a plagioclase/clinopyroxene/Fe-rich groundmass and of zeolite filled vesicles
Gdm-microlitic
Gdm-Pl,Cpx,Fe
Ves
Ves
Ves
lichenous patina
Ves

## Slide 35: Figure4. 2b vesicle-filling anhedral analcime (Na16[Al16Si32O96] 16H2O)
analcime

## Slide 36
Fig.4.2c) vesicle filling acicular natrolite (Na16[Al16Si24O80] 16H2O)
natrolite

## Slide 37: Fig.4.2f) vesicle filling smectitic clay
Smectitic

## Slide 38
Fig.4.4g) biofilm, extracellular polymeric substances (EPS) coating crystalline Fe/Ti oxides
biofilms (which more than often act as signs to the subsequent development of stone surface covering lichenous mats and are widespread in Lalibela, (fig.4.4g)

## Slide 39: XRD analysis
XRD
zeolites (in order of peak strength: analcime, heulandite)
Clinopyroxene
Pyroxene
Hematite
Calcite
Sanidine
Plagioclase
and minor smectites

## Slide 40: 4.2 Fourier Transform Infrared and Raman Spectroscopic Analysis of Clay Minerals

## Slide 41
4.2.1 FTIR analysis
FTIR analysis comparing the observed frequencies with the available literature, secondary minerals such as
Calcite-CaCO3
Montmorillonite-(Na, Ca)x(Al, Mg)2(Si4O10)(OH)2+nH2O
Gypsum-CaSO4 +2H2 O
Magnetite- Fe3 O4
Hematite-Fe2 O3
Kaolinite-Al2 Si2 O5 (OH)4
Whewellite-CaC2 O4 + H2 O
Weddellite- CaC2 O4 + 2H2 O
was identified.

## Slide 42
Sample | Kao. | Mont. | Cal | Gy | Hm. | Mgt. | Ww. | Wd.
Bs | 3694 3619 1031 444 | 3427 1642 | 2514 1799 1421 876 712 | ̶ | ̶ | ̶ | 1320 | ̶
B4 | 1032 438 | 3435 1628 | 2513 1799 1421 876 711 | ̶ | ̶ | ̶ | ̶ | ̶
Table4. 1 Absorption Frequency in the region of 4000 – 400 cm-1 of the bulk basalt of Lalibela, together with minerals identification. (Kao= Kaolinite, Mont= Montmorillonite, Cal= calcite, Gy= gypsum, Hm= hematite, Mgt= Magnetite, Ww= whewellite, Wd= Weddellite)

## Slide 43: Table4. 2 Absorption Frequency in the region of 4000 – 400 cm-1 of the bulk tuff of Lalibela, together with minerals identification. (Kao= Kaolinite, Mont= Montmorillonite, Cal= calcite, Gy= gypsum, Hm= hematite, Mgt= Magnetite, Ww= whewellite, Wd= Weddellite)
Sample | Kao. | Mont. | Cal | Gy | Hm. | Mgt. | Ww. | Wd.
Ts | 3677 1034 | 1637 | ̶ | 3541 3406 1671 1622 1140 1116 670 603 | 540 | 582 | 1311 | 1355
T4 | 1043 | 3434 1638 | ̶ | ̶ | 539 | 578 | ̶ | ̶

## Slide 44: Table4. 3 Absorption Frequency in the region of 4000 – 400 cm-1 of the samples collected from internal and external walls of rock hewn churches of Lalibela, together with minerals identification. (Kao= Kaolinite, Mont= Montmorillonite, Cal= calcite, Gy= gypsum, Hm= hematite, Mgt= Magnetite, Ww= whewellite, Wd= Weddellite).
Sample | Kao | Mont | Gy | Hm | Mgt | Ww | Wd
TG-M | 1035 1016 448 | 1638 520 | 3410 674 603 | ̶ | 579 | ̶ | ̶
BGR-I | 3676 1031 | ̶ | 3538 3406 1622 1685 1115 671 602 | ̶ | 579 | 1326 | 1354
BGS-E | 1032 444 | 3427 1632 | 3415 670 | 536 | 583 | 1324 | ̶
BMG-E | 1035 445 | 3434 1639 | ̶ | ̶ | 580 | 1315 | 1356
BGM-B | 3681 1039 444 | 1643 | 3533 3401 | 533 | ̶ | 1322 | ̶
BGM-R | 1040 444 | 1639 | 3534 3408 | 540 | ̶ | 1323 | ̶

## Slide 47: Infrared absorption frequencies and Probable assignment of rock samples of Lalibela rock hewn churches
(cm-1) | Mineral Name | Tentative Assignment | Reference
3690 | Kaolinite | Inner surface OH Stretching vibration | [ ]
3620 | Kaolinite | O-H- Stretching of inner hydroxyl | [ ]
1034 | Kaolinite | Si-O-Stretching of clay mineral | [ ]
3434 | montmorillonite | O-H- Stretching of absorbed water molecule | [ ]
1642 | montmorillonite | H-O-H- bending vibration of absorbed water molecule | [ ]
1322 | whewellite | metal-carboxylate stretch, νs (COO–) | [ ]
1355 | weddellite | metal-carboxylate stretch, νs (COO–) | [ ]

## Slide 48: Raman analysis
absorption intensity of the samples are compared with the reference samples, marble and quartz. The peak intensities of the samples are highly associated with the marble reference
The intense band (ν1) of calcite spectrum corresponds to the symmetric stretching of CO3 group at 1077 cm-1. The ν2 (asymmetric deformation) vibration mode is not active in Raman. The values attributed to ν3 (asymmetric stretching) mode are 1428 cm-1 and ν4 (symmetric deformation) mode at 706 cm-1

## Slide 49: µ-Raman analysis
Micro Raman on the tuff sample confirmed the extensive laterization experienced by the basaltic pyroclastic scoria deposit with the identification (beside peaks attributable to zeolitic (analcime) minerals) of well-defined peaks of
hematite,
lepidocrocite and
combined hematite/lepidocrocite
The positions of the hematite spectral peaks are shown at 227, 293, 409, 499, 609cm-1
the Raman spectrum of lepidocrocite (γ-FeOOH) exhibits a broad band about 1312cm-1.

## Slide 50: Table4. 4 Elemental composition of rock samples of Rock hewn churches of Lalibela (Mean % weight)
 | BGM |  | Basalt |  | Tuff | 
Element | Mean % weight |  | Mean % weight |  | Mean % weight | 
C O Na Mg Al Si P S K Ca Ti Fe | 9.71 43.77 1.70 3.06 3.90 12.33 0.78 1.17 2.50 6.33 2.65 15.32 |  | 13.35 45.62 -- 1.98 3.01 10.99 -- -- 3.45 14.2 1.79 6.21 |  | 11.02 45.27 2.79 2.23 4.86 13.43 0.78 -- 0.56 5.11 2.1 11.84 | 
Sample basalt appears to be particularly C and Ca rich, sample tuff contain high quantity of Na, sample BGM contains more Fe and S than the other samples.
From the EDS analysis, the abundant amount of Si, Al, Ca, Mg, Fe, K and Ti was founded and it supports the vibrational spectroscopic findings; the presence of
aluminosilicates (Si, O, Al, K, Na, Mg), Fe-rich oxide (Fe–O) and gypsum (Ca–S–O)
SEM-EDS analysis

## Slide 51
White tie
Dark area
Clear grains

## Slide 52
White phases-1
White phases-2
Dark matrix

## Slide 53: 4.3 Analysis of Rock Samples Using Laser-Induced Breakdown Spectroscopy

## Slide 54
Analysis of Samples
The LIBS signal from
bulk (clean) stones was
five consecutive laser shots -in two different sites (total ten spectra).
The powder pellets,
ten consecutive shots applied at four different sites (total forty spectra)
The spectral lines considered are listed in Table 4.5 and
typical examples of the spectra measured from encrustation (powder) and bulk (clean) rock samples, with the most intense lines identified, are shown in Fig.4.21-Fig.4.23

## Slide 55: Table4. 5 elements detected from the encrustation and the bulk rocks
Wavelength(nm) | Element | Wavelength(nm) | Element
274.63 | Fe(II) | 422.81 | Ca(I)
279.27 | Mg(II) | 643.8 | Ca(I)
284.95 | Mg(I) | 656.4 | H(I)
287.88 | Si(I) | 670.7 | Li(I)
315.96 | Ca(II) | 766.4 | K(I)
318 | Ca(II) | 777.26 | O(I)
323.5 | Ti(II) | 396.18 | Al(I)
407.31 | Fe(I) | 589.01 | Na(I)
407.88 | Sr(II) | 249.62 | B(I)
455.47 | Ba(II) | 403.08 | Mn(I)

## Slide 57: Composition differences of the powder samples and the bulk rock
To compare the composition of bulk and powder samples, we have normalized all line intensity on N line at 744.2nm
The major rock-forming elements include Si, Al, Fe, Mg, Ca, Na, K, and Ti. The relative abundances of these elements can be used to assess the conditions and extent of weathering that a surface has experienced.
Their mobility relative to one another are dependent on the primary phases from which they are released and the secondary phases in which they are present.

## Slide 59
Selected LIBS spectra obtained within the encrustation at different laser shot corresponding to the different depths from the surface of basalt altered is presented.
For a better presentation of the spectra -normalized, with respect to the intensity of the N line at 744.2nm. Nitrogen comes mainly from air and is suitable for the normalization of the elements, and helps to see the differences clearly
In this way it was possible to observe surface impurities and find out their disappearance in depth
.
Depth profiling

## Slide 60
We compared the intensity ratio of hydrogen on the powder, bulk rocks and during the depth profiling of the weathered basalt samples.
Hydrogen emission peak (656.4nm) was first normalized on the nearby line intensity of Ca (643.8nm), belonging to the same spectrometer channel.
H/Ca intensity ratio is higher in the samples collected from external wall of the churches i.e. exposed to the wetting.
The emission from H in weathered basalt was detected for all laser shots, with the maximum corresponding to the seventh shot.
The presence of hydrogen is the indicator of humidity in dirty layer.
high detected presence in the powder samples, is an indicator of dissolving feldspars into secondary minerals, (as for example kaolinite and montmorillonite caused by hydration of inorganic cations.
It is suggested that replacement of cations with H+, involves a weakening of the crystal structure and hence a loss of strength of the crystals because:
(1) the replacement cations have different valences from the original cations, creating a charge imbalance; and
(2) the ionic radii of the replacement cation (H+ = negligible) is smaller than those of the original cations

## Slide 61: Sample classification
Comparison between the line intensities of the elements forming samples allows classification of the mineral type. This is demonstrated in Table, where the names and correlation coefficients for the rock samples with the most related LIBS spectra are listed for the 7 analyzed samples (rock and powder).
The correlation coefficient line intensity
Bete Gebriel Rufael-external- Bete Mikeal Golgotha-external
r=0.99443
Bete Gebriel Rufael-internal- Bete Gebriel Rufael-external
r = 0.88465
suggesting that it would have been, samples colonized by similar deposits (lichens, green algae, and various fungi), the rock-forming minerals of these samples are transformed into secondary minerals, plus the difference in substrate composition of the rock exterior and interior of the churches

## Slide 62
Sample
Tuff 1
Basalt 0.89328 1
BGR-E 0.72649 0.84112 1
BGR-I 0.87257 0.85304 0.88465 1
BG-E 0.80562 0.9335 0.96874 0.90548 1
BG-I 0.86781 0.90659 0.89451 0.96577 0.9351 1
BMG-E 0.74997 0.87319 0.99443 0.89688 0.98573 0.91065 1
Tuff Basalt BGR-E BGR-I BG-E BG-I BMG-E

## Slide 63: Figure4. 38 Correlation between selected peak line intensities from the spectra of samples from a) external and internal wall of Bete Gebriel Rufael b) basalt (bulk) and Bete Giyorgis-external (BG-E). The linear correlation coefficient r is given on the plot.
The peak intensity of the network below the regression line shows relatively uniform distribution between the two samples
the data above the regression line records a peak intensity of the network that has highest in the sample Bete Gebriel Rufael internal (BGR-I)
In this comparative study LIBS line intensity among the elements that constitute the samples allows to classify the type of mineral.

## Slide 64: Conclusion

## Slide 65
the combined microscopical/chemical study highlights for the first time the major role played by epilithic and endolithic lichen colonization in the surface weathering of the Lalibela stones.
Lichen induced biodeterioration operates both via biogeophysical (hyphae contraction/swelling) and biogeochemical (acidolysis/dissolution and metal complexation) processes.
Metal extraction (Fe, Mg, Al) as a source of energy and as a nutrient supply seems to particularly active on clinopyroxene minerals. These decay processes act more active in causing severe desegregation of the stone fabric with the inglobation of mineral fragments from the stone substrate into the growing biological patina.
The high porosity of the volcanic scoria deposits in Lalibela coupled with their mineralogical heterogeneity (which may produce bacterial communities with unprecedented richness of species) provides the most favourable conditions for lichen and bacterial colonisation and associated bio-induced decay. Once established, these patinas may act as preferential sites for water absorption/retention further accelerating both bio and/or salt weathering mechanisms.

## Slide 66
The IR spectroscopic analyses of rock samples from the rock hewn churches of Lalibela indicate the presence of secondary minerals zeolite-group, calcite, kaolinite, whewellite/weddellite, montmorillonite, gypsum, magnetite, lepidocrocite and hematite. Among the different secondary minerals, montmorillonite is present more or less in all samples, however, gypsum and calcite, were the most abundant minerals in samples tuff (Ts), BGR-I and bulk basalt, respectively.
The presence of zeolite, smectite (montmorillonite) are reported by other workers as the sources of the progressive deterioration of the geomechanical properties of the rocks in Lalibela.
In the present study we bring attention to the presence of kaolinite, gypsum, lepidocrocite and whewellite/weddellite not identified before on the rock hewn churches of Lalibela, besides the presence of montmorillonite in depth of bulk samples.

## Slide 67
This study also demonstrates that LIBS spectra can be used to match rock samples collected from the inner and outer walls of rock-hewn churches of Lalibela. Comparing mediated LIBS spectra against each other and with tuff and basalt samples. The samples collected from the outer wall of the churches are well correlated.
Selected LIBS spectra obtained within the encrustation at different laser shots corresponding to different depth from the surface of weathered basalt is presented.
A causal relationship between the relative loss of cations and higher presence of hydrogen in the samples collected from external wall of the churches and in-depth profile of weathered basalt is suggested. Cations are lost from the constituent primary minerals and replaced by H+; this process disrupts the lattice structure and causes a marked loss of strength.
This study suggests that LIBS is also the promise of identifying impurities characteristics of the rocks and their deposits.

## Slide 68: Recommendations

## Slide 69
Results indicate that biological attack by green algae and lichens is currently responsible for severe stone surface, physical and chemical weathering leading to considerable weakening of the churches walls. A prompt and careful removal of the biological and other deposits with the non-destructive method (laser cleaning) treatment is available therefore further investigation on laser cleaning of the deposits is recommended,
investigation on the influence aspect, exposure and nature of bioinfestation(eg. pest organisms) on the rock hewn churches of Lalibela.

## Slide 70
THANK YOU for Your Patience